## Slide 1: Nuclear waste vitrification efficiency: cold cap
Pavel Hrma
Albert A. Kruger
Richard Pokorný

## Slide 2: Hanford site
Manhattan project
Washington, USA
B – reactor
  1. nuclear reactor
  Plutonium production (World War II.)
Peak production reached during cold war
  9 running nuclear reactors
The legacy of Pu production: Nuclear waste
Today – clean up process

## Slide 3: Nuclear waste
177 underground tanks
206 630 m3 of nuclear waste

## Slide 4: Waste treatment plant (“Vitrification plant”)
Vitrification
  Immobilization of the waste in the form of glass
  Waste + Glass forming additives --> heated to 1150 C
  The melt then poured to stainless steel canisters to cool and solidify
  In this form, the waste is stable and safer for the environment
Current state (February 2011)

## Slide 5: Glass melting
Waste glass melter – a schematic image
Slurry feed
Electrodes
Molten glass
Cold cap
Bubbler

## Slide 6: Mathematical modeling of cold cap
Final goal – implementation of the cold cap mathematical model to the glass melter model
  Mathematical models of melters are commonly used for the simulation of melter behavior under different conditions
Slurry feed
Molten glass
Cold cap

## Slide 7: Mathematical modeling of cold cap
The feed is charged into the melter in the form of slurry containing 50 to 60 mass% of water.
Water is boiling and evaporating on the top of the cold cap.
The cold cap of nearly uniform thickness is spreading over the pool of molten glass.
Only enough feed is being charged to maintain a cold cap that covers ~90% of the surface.
  Should not cover more than 95% from technological reasons
Slurry feed
Molten glass
Cold cap

## Slide 8: Mathematical modeling of cold cap
As the feed materials move down through the cold cap, their temperature increases from 100˚C to the temperature of molten glass (1100˚C).
The batch reactions include
water evaporation,
release of bonded water (crystalline water, water from hydroxides , oxyhydrates, and boric acid),
melting of oxyionic salts and borates,
  reaction of nitrates with organics,
  molten salt migration,
  reactions of melts with amorphous oxides and hydroxides,
  reaction of molten salts with solid silica,
formation of intermediate crystalline phases (e.g., spinel),
formation of a continuous glass-forming melt,
  volatilization,
  expansion and collapse of foam,
  dissolution of residual solids (mainly silica).

## Slide 9: Cold cap structure
x is the vertical coordinate
h is the cold cap thickness
Simplifications:
  1D representation
  2 phases
    condensed phase
    gas phase

## Slide 10: Mathematical modeling of cold cap
The development of the algorithm to calculate the 1D temperature field in the cold cap:
  Mass balance + Energy balance
  Constitutive equations for material properties
  Boundary conditions
Finite difference method was chosen for its simplicity and comprehensibility

## Slide 11: Mass balance
Neglecting the diffusion, the mass balances of the condensed phase and the gas phase are
By the mass conservation law, the total mass balance is
  ρ is the spatial density
  v is the velocity
  r is the mass change rate (via chemical reactions)
  subscripts c and g denote the condensed phase and the gas phase, respectively

## Slide 12: Energy balance
In a steady state, the energy balance equations are
By the Fourier’s law, the conductive heat fluxes are:
c is the heat capacity
q is the conductive heat fluxes
H is the heat source/ sink due to chemical reactions
s is the heat transfer between gas phase and condensed phase
subscripts c and g denote the condensed phase and the gas phase, respectively

## Slide 13: Boundary temperatures and fluxes
QU and QB are the heat fluxes
TU and TB are the boundary temperatures

## Slide 14: Material properties
A typical HLW melter feed has been chosen
  Its properties, such as heat capacity, were measured or estimated based on the literature

## Slide 15: Results preview
QU is the heat flux delivered to the cold cap from above
  QS is the heat flux to convert the slurry to 100˚C (~60% of total heat flux for melting)
Effect of upper heating on the cold cap thickness
  The cold-cap thickness decreases as the total heat flux delivered to it increases
  The more heat is delivered from above, the thicker the cold cap becomes
Total heat flux to cold cap in kW m-2

## Slide 16: Foam layer
Picture of bubble layer structure under cold cap
X-ray tomography image of foam after melting
Picture of bubble layer structure under cold cap
X-ray tomography image of foam after melting
Expansion experiments show presence of foaming

## Slide 17: Foam layer models
Structure of foam layer
Understanding of foam is essential for the cold cap modeling

## Slide 18: Conclusions
The preliminary 1D model of the cold cap has been developed
The thickness of the cold cap decreases as the feat flux to the cold cap increases and increases as the fractional heat flux from above increases
Empirical data indicate that foaming has a strong impact on the melting rate
Further experimental investigation and mathematical modeling of foaming is underway